# SYKON SL450s – Thermal Break Sliding System

## Technical Catalogue

## 1. System Overview

SL450s is a thermal break sliding door and window system designed for residential and commercial applications.

The system supports:

- Sliding doors and windows

- Monorail Configuration (Fixed – Slide)

- Double Rail up to 5-Rail Configuration

- Embedded Sill with Gutter Profile

- Fixed and operable sidelights

- Multiple panel configurations

It incorporates slim interlock design, smooth sliding performance, and compatibility with integrated façade systems.

## 2. Performance Summary

| Performance Item | Standard | Result | Status |
| --- | --- | --- | --- |
| Air infiltration / exfiltration | ASTM E283 | 600 Pa | Pass |
| Water penetration | ASTM E331 | 600 Pa | Pass |
| Wind resistance – serviceability | ASTM E330 | 1920 Pa | Pass |
| Wind resistance – safety | ASTM E330 | 2880 Pa | Pass |

## 3. Measured Performance Data (Representative Sample)

| Parameter | Value |
| --- | --- |
| Air infiltration @ +300 Pa | 7.1 m³/h |
| Air infiltration @ +450 Pa | 9.8 m³/h |
| Air infiltration @ +600 Pa | 11.4 m³/h |
| Air exfiltration @ -300 Pa | 3.3 m³/h |
| Air exfiltration @ -450 Pa | 4.6 m³/h |
| Air exfiltration @ -600 Pa | 5.6 m³/h |
| Static water penetration (390 Pa) | No water ingress |
| Static water penetration (600 Pa) | No water ingress |
| Wind resistance | No visible damage |
| Deflection limit | Within L/175 |

## 4. Wind Deflection (Representative Values)

### Serviceability Load

| Parameter | Value |
| --- | --- |
| Peak deflection | +7.6 mm / -7.1 mm |
| Residual deflection | +0.1 mm / -0.2 mm |
| Allowable limit | Within permissible |

### Safety Load

| Parameter | Value |
| --- | --- |
| Residual deflection (measured) | ±0.2 mm |
| Allowable residual | 4.6 mm |
| Structural integrity | No failure |

## 5. System Basic Technical Data

| Item | Value |
| --- | --- |
| System type | Sliding door / window system |
| Frame width | 104 mm (minimum) |
| Sash height | 75 mm |
| Interlock width | 30 mm |
| Aluminium alloy | EN AW 6063 (AlMgSi) |
| Hardness | 12 – 14 HB |
| Profile thickness | 1.4 – 6.0 mm |
| Thermal break | Polyamide PA 6.6 |
| Maximum panel weight | 200 kg |
| Glazing type | Single / Double |
| Maximum glazing thickness | Up to 28 mm |
| Powder coating thickness | Min. 75 microns |

## 6. Rail / Frame Profile Options

| Profile | Width (mm) | Weight |
| --- | --- | --- |
| C450-150 | 86 | 1518 gr/m |
| C450-151 | 104 | 1833 gr/m |
| C450-250 | 75 | 1254 gr/m |
| C450-450 | 36.6 | 765 gr/m |

Additional profiles:

- P450-602 (side profile)

- P450-611 / 623 / 624 (rail accessories)

## 7. Sash Profile Options

| Profile | Dimension (mm) | Weight |
| --- | --- | --- |
| P450-620 | 50 × 20.5 | 633 gr/m |
| P450-621 | 30 × 20.5 | 484 gr/m |
| P450-606 | 36.6 × 22 | 396 gr/m |

## 8. Interlock / Meeting Stile Options

| Profile | Width (mm) | Weight |
| --- | --- | --- |
| P010-100 | 61 | 2012 gr/m |
| P010-160 | 61 | 3162 gr/m |

## 9. Glazing Range

| Configuration | Thickness Range |
| --- | --- |
| Single glazing | Supported |
| Double glazing | Supported |
| Maximum glazing thickness | Up to 28 mm |

### Typical Tested Configuration

- 28 mm DGU (6 mm + 16 mm gap + 6 mm)

## 10. Hardware & System Components

### Rollers

- 25 mm heavy-duty adjustable double rollers

- Teflon material (high durability and smooth operation)

### Locking Options

- Single-point locking

- Multi-point locking

- Backset locking integrated within sliding guide

### Additional Options

- Flyscreen compatibility

- Interlocking profiles

- Meeting stile configurations

- Integration with SYKON S60 systems

## 11. Gaskets & Sealing Components

| Component | Description |
| --- | --- |
| G2002 | Pocket jamb gasket |
| G2003 | Slim interlock gasket |
| WG20–WG70 | Wedge gaskets (2 mm – 7 mm range) |
| WP06 / WP07 | Weather pile (6 mm / 7 mm) |

## 12. PVC / Auxiliary Profiles

| Profile | Description |
| --- | --- |
| PP2009 | Basin profile |
| PP2008 | Slim interlock PVC |
| PP2002 | Rail basin cover (optional) |

## 13. System Behavior

- Designed for smooth and low-friction sliding operation

- Integrated thermal break system for insulation performance

- Efficient water drainage and outflow design

- Multi-component sealing system ensures:

  - Air tightness

  - Water resistance

  - Acoustic performance

## 14. System Options

- Monorail Configuration (Fixed – Slide)

- Double Rail up to 5-Rail Configuration

- Embedded Sill with Gutter Profile

- Fixed and operable sidelights

- Multiple panel configurations

- Flyscreen integration and / or as add-on profile

- Interlocking and meeting stile variations

## 15. Area of Usage / Project Type

Suitable for:

- Residential villas and apartments

- Commercial buildings

- Balconies and terraces

- Sliding façade systems

- Mixed-use developments

## 16. Key Technical Highlights

- Thermal break sliding system

- Slim 30 mm interlock design

- Supports panels up to 200 kg

- Smooth operation with heavy-duty rollers

- Glazing up to 28 mm

- Multiple configuration flexibility

- Integrated locking and sealing systems